## Slide 2: Problem Statement
The responses of a LRC circuit driven by an AC source can be changed by inserting either a non-magnetic metal rod or a ferromagnetic rod into the inductor coil. How can we obtain the magnetic and electric properties of the inserted rod from the circuit’s responses?

## Slide 3: Basic physics
coil1.gif (600×340) (nde-ed.org)
Inductor coil + AC current  changing magnetic field (magnetic induction)
Inserted rod interacts with this field
  extra currents generate
  magnetic field weakens/strengthens
Properties of the inductor change
Process:
  measure the steady-state response of the circuit
  circuit theory  acquire the properties of the inductor
  electromagnetic theory  calculate the properties of the rod
Notes: electromagnetic phenomenons happen

## Slide 4: I. LRC theory

## Slide 5: LRC circuit components
changes when inserting the rod
Driving AC voltage:
Inductor:
  resists the change of current
  voltage goes in front of current ()
Resistor:
  no phase difference between U and I
Capacitor:
  resists the change of voltage
  voltage lags behind current ()
Notes: reactance – resistance-like property

## Slide 6: Circuit diagram

## Slide 7: Circuit response – steady state
Voltage (V)
Time (s)
Notes: measured through a frequency spectrum

## Slide 8: Basic equations
Phase angle formula:
From Ohm’s law:
Z: impedance
X: reactance

## Slide 9: Voltage ratio graph
At resonance frequency:
changing L or C
changing RL or R
Notes: plot legyen!

## Slide 10: Phase angle graph

## Slide 11: II. Measurement setup

## Slide 12: Setup – inductor
Inductor:
  N = 1200
  L0 = 0.028 H
  R0 = 16.4 Ω
  l = 5 cm
  d = 1.9 cm
U0 = 2.5V (sinusoidal)
Notes: több kondi és elllenállás

## Slide 13: Resistors and capacitors
C1 = 272 pF
C2 = 350 pF
C3 = 4.71 nF
R1 = 289 Ω
R2 = 480 Ω
R3 = 1041 Ω

## Slide 14: Rods
Rod materials:
  Aluminium (Al)
  Copper (Cu)
  Iron (Fe)
Drilled holes
non-magnetic conductors
ferromagnetic

## Slide 15: Instruments
XDG 3162 Function generator
DSO 4022 Oscilloscope

## Slide 16: III. Results

## Slide 17: Voltage ratio for different materials

## Slide 18: Different resistors
Ω
Ω
Ω
Ω
Ω
Ω
aluminium is similar to copper
Only the height of the peaks changes!
small ratio 
RL is greater

## Slide 19: Different capacitors
Resonance frequency changes, but height too!
RL somehow changes
frequency dependent

## Slide 20: How do the properties of the core influence L and RL?

## Slide 21: Magnetic field in an ideal coil
(current out)
(current in)
μr: relative permeability of rod , N: number of loops of coil , A: cross-section of rod
Magnetic flux of the coil:
Magnetic field:
AC source
magnetic field constantly changes

## Slide 22: Eddy currents in the core
Faraday’s law of induction:
Voltage + closed loop in the core 
Lenz’s law  IEddy opposes IL
Eddy-currents will flow
L: inductance of coil
Eddy currents induce magnetic fields
concentric currents  Bind grows towards the center
Notes: … the magnetic field constantly changes. So does the magnetic flux …

## Slide 23: Skin effect
opposite Eddy-currents
B = B0cos(ωt)
Bind weakens the original B 
total B exponentially decays – decay rate is the skin depth
magnetic field can only penetrate in the rod until a given distance
Sci-Hub | Formulas for the Skin Effect. Proceedings of the IRE, 30(9), 412–424 | 10.1109/jrproc.1942.232015
grafikon a különböző B terekről

## Slide 24: Skin-depth δ
Eq for B decay – delta definition (decay rate)
Fluxus kiintegrálva?
Effective magnetic flux:
σ: conductivity of rod ; ρ: resistivity of rod
(for )
δ
Notes: EGYENLETEK!!!

## Slide 25: Skin depth (example)
δ (mm)
f (Hz)
Aluminium
Copper
Iron
Measuring range:
8 000 – 100 000 Hz
Notes: szebb plot – delta eq.val

## Slide 26: Experiments – hole in the core
Notes: új plotok

## Slide 27: V. Inductivity and resistance of coil

## Slide 28: Inductivity
(electromagnetic induction)
The same ratio can be expressed from the change of resistance of the coil – irrelevant.
képek
electric and magnetic properties arise:
Notes: permeability and conductivity can’t be separated

## Slide 29: Currents in the core
IL
Itube

## Slide 30: Heat loss
resistance of the wires is constant (a bedugáskor!) 
Joule-heating in the core:
Notes: nem az a delta

## Slide 31: Electric and magnetic properties
Constant for the coil:
From L:
From deltaR:
Notes: A*m / V*s odaírni MÉRTÉKEGYSÉG!!!

## Slide 32: VII. Comparison, accuracy

## Slide 33: Comparison
literature range
measurements
Notes: különböző módokat más-más dián?

## Slide 34: Accuracy
különböző paramétereknél hogy javul/romlik az eredmény

## Slide 35: VII. Summary

## Slide 36: Summary
Procedure:
  Measure both peak voltages and the phase
  Calculate L and RL through curve fitting
  Solve the resulting equation system

## Slide 37: Summary
Thank you for your attention!

## Slide 38: Structure
problem statement, basic physics
theory I – RLC circuit
RLC measurement setup
evaluation  L and dR
theory II – Maxwell, obtaining σ and μ
relevant params, prooving skin depth
comparison – limitations
summary – whole process

## Slide 39: Appendix – different resistors
Notes: új plottok, mik változnak, képlettel – beszélni a plotokról! – frekvencia függés bevezetése

## Slide 40: Appendix – different capacitors
Notes: új plottok, mik változnak, képlettel – beszélni a plotokról! – frekvencia függés bevezetése

## Slide 41: Appendix – phase angle measurement

## Slide 42: Appendix – electric and magnetic properties
Material | Relative permeability | Conductivity (S/m , 20°) | Temperature coefficient
Al | 1,000022 | 3,77 e7 | 3,9 e-3
Cu | 0,999994 | 5,96 e7 | 4,04 e-3
Annealed Cu |  | 5,8 e7 | 3,93 e-3
Fe (98% pure) | 5000 - 200000 | 1,03 e7 | 5 e-3
Steel | 100 - 38000 | 1,45 e6 – 6,99 e6 | 
Sources:
Appendix 8: Electrical Conductivity of Selected Materials - An Introduction to Materials Engineering and Science - Wiley Online Library
Electrical resistivity and conductivity – Wikipedia
Permeability (engineeringtoolbox.com)

## Slide 43: Appendix – sources
  2560px-Inductor_symbol.svg.png (2560×640) (wikimedia.org)
  capacitor-symbol.jpg (600×200) (wiltronics.com.au)
  2560px-Resistor_symbol_Europe.svg.png (2560×1280) (wikimedia.org)
  360_F_508722395_Pl3TdrRJjGBqpwcFETTLJf3xlWi9D09I.jpg (360×360) (ftcdn.net)
  0 (976×385) (mtstatic.com)

## Slide 44: LRC circuit components
changes when inserting the rod
Driving AC voltage:
Inductor:
  resists the change of current
  voltage goes in front of current ()
Resistor:
  no phase difference between U and I
Capacitor:
  resists the change of voltage
  voltage lags behind current ()
Notes: reactance – resistance-like property

## Slide 45: Phasor diagram
Reactance and resistance – phasors
Impedance (vector sum):
φ angle – phase difference between U and I:
steady-state response
Notes: érdekesebb, egyszerűbben érthető legyen, több BASIC physics

## Slide 46: Equations – simple LRC theory
geometry
Ohm’s law

## Slide 47: Appendix – long rod
72 500 Hz
72 600 Hz
72 400 Hz
The ratio of voltages and resonance frequency should not change!
Notes: mielőtt kifúrtuk…

## Slide 48: Appendix – skin effect illustration

## Slide 49: Appendix – proximity effect

## Slide 50: Appendix – magnetic hiszterézis

## Slide 51: Appendix – ferromagnetism vs. ferrimagnetism
Ferromagnetism – Wikipedia, Ferrimagnetism – Wikipedia – 1948, Louis Néel
Ferrite:
  Relative permeability: 10 – 20000
  very low conductivity
Ferrite | Iron Oxide Compound | Britannica

## Slide 52: Electric and magnetic properties
Material | Resonance frequency [Hz] | L [H]
Al | 72 300 | 0,0178
Cu | 72 500 | 0,0177
Fe | 56 200 | 0,0295
Ratio (
Constant for the coil:
Notes: A*m / V*s odaírni MÉRTÉKEGYSÉG!!!